RedLam™ LVL Specifications

1.0 GENERAL

1.1 Scope

This work includes the complete furnishings and installation of all RedLam™ laminated veneer lumber (LVL), as shown on the drawings herein specified and necessary to complete the work.

1.2 Code Approvals

These products shall be designed and manufactured to the standards set forth in the ICC ES Report No. ESR-2993.

1.3 Related Work Specified Elsewhere

- Carpentry and Millwork

- Glu-Laminated Members

1.4 Design

- Products:  RedLam™ LVL shall be designed to fit the dimensions and loads indicated on the plans.

- Design Calculations:  When requested, a complete set of design calculations shall be prepared by RedBuilt™.

1.5 Submittals

- Drawings:  When requested, drawings showing layout and detail necessary for determining fit and placement in the building shall be provided by RedBuilt™.

- Production:  Fabrication and/or cutting shall not proceed until the architect and/or engineer have approved the submittal package.

2.0 PRODUCTS

2.1 Materials

- Code Reports:  Materials shall comply with ICC ES Report No. ESR-2993.

- Adhesives:  Adhesives shall be of the waterproof type conforming to the requirements of ASTM D-2559.

2.2 Fabrication

RedLam™ LVL shall be manufactured by RedBuilt™ in a plant listed in the report referred to above and under the supervision of an approved third-party inspection agency.  It shall be manufactured in a continuous process, with all grain parallel with the length of the members. All members are to be free of finger joints, scarf joints, or mechanical connections in full-length members.

2.3 Tolerances

Finished Length (as specified): ± 1/8"

Depth: ± 1/16"

Width: ± 1/16"

2.4 Identification

RedLam™ LVL shall be identified by a stamp indicating the product type and grade, ICC-ES evaluation report number, manufacturer's name, plant number, date of fabrication, and the independent inspection agency’s logo.

2.5 Hardware

Not applicable.

3.0 EXECUTION

3.1 Installation

RedLam™ LVL, if stored prior to installation, shall be protected from the weather. It shall be installed in accordance with the plans, and any RedBuilt™ drawings and installation suggestions. Temporary construction loads that cause stresses beyond design limits are not permitted. Safety bracing is to be provided by the installer to keep the RedLam™ LVL straight and plumb as required, and to ensure adequate lateral support for the individual RedLam™ LVL members and the entire system until the sheathing material is applied.

3.2 Installation Review

Prior to enclosing RedLam™ LVL, the contractor shall give notification to the RedBuilt™ representative to provide an opportunity for review of the installation.

3.3 Performance Standards

Products shall be proven by testing and evaluation in accordance with the provisions of ASTM D-5456.

3.4 Fire Rating

RedLam™ LVL is permitted as a substitute for conventional wood framing in fire-resistive assemblies. RedLam™ LVL shall be sized for the same load-carrying capacity as the sawn lumber specified in the assembly, and its dimensions shall be equal to or greater than those specified for the sawn lumber.

3.5 Warranty

The products delivered shall be free from manufacturing errors or defects in workmanship and material.  The products, when correctly installed and maintained, shall be warranted to perform as designed for the normal and expected life of the building.

4.0 ALTERNATES AND/OR EQUALS

4.1 Base Bid

Due to the customized detailing and engineering characteristics of the roof and/or floor framing assembly, it is a requirement that RedLam™ LVL be used in the base bid.

4.2 Alternate Manufacturers

Other manufacturers’ bids are to be listed in the alternate section of your proposal.  All framing plans, detailing, and calculations for the alternate bids will be reviewed by the owner, architect, and engineer for structural performance, possible conflicts with related trades, and compatibility with the overall building requirements and building code.

4.3 Alternate Products

Alternate products will only be permitted if written approval and acceptance is obtained by both architect and owner at least seven (7) days prior to the bid date.  Any monetary savings that may be realized by using an alternate product shall be forwarded to the owner.

4.4 Acceptable Alternates

At the discretion of the specifier of record, accepted alternates will be listed on the final addendum prior to the bid date.